Carbon Steel Galvanized OnGrip®

OnGrip® Spray Traction Surface, as manufactured by Ohio Gratings, Inc. (800-321-9800) www.ohiogratings.com, is applied to carbon steel plate and grating after surface blasting to remove mill scale and other surface contamination. The metal spray surface has a high bond strength exceeding 4,000 psi.  However, special care must be exercised during the hot-dip galvanizing process per ASTM A123 to avoid potential damage to the OnGrip® surface.

Customers are strongly encouraged to allow Ohio Gratings, Inc. to take responsibility to control the galvanizing process, and ship the grating and plate products complete with finish, ready for installation.  When this is not possible, we offer the following recommendations to be adhered to with extreme caution, especially in the absence of experience in galvanizing this product:

- Any other carbon steel material to be welded to the OnGrip® products should be blast cleaned to remove all mill scale and rust prior to fabrication, assembly and galvanizing.

- Materials with OnGrip® surface must be kept dry prior to galvanizing to avoid any surface rust formation.

- Acid pickling time is critical and should be limited to 10 minutes maximum, dependent on the concentration of the ambient temperature hydrochloric acid solution. Do not use sulfuric acid solution for this application.

- Hot spots during the pickling process must be avoided by maintaining sufficient space between products.

- The zinc bath temperature should be maintained between 830°F and 840°F. However, there are variables that will affect the ideal temperature.

- Airblast is recommended to remove excess zinc from the OnGrip® surface.

Ohio Gratings, Inc. strongly recommends that Canton Galvanizing, LLC (contact information below) be engaged to perform the hot-dip galvanizing process on all products that include OnGrip®.  This firm has special expertise and excellent process controls to ensure the quality of the ASTM A123 hot-dip process and the traction surface.

Canton Galvanizing, LLC

1821 Moore Ave SE, Canton, OH 44707

Phone: 330-685-9060

The customer is responsible for the OnGrip® galvanized finish if Ohio Gratings, Inc. or Canton Galvanizing are not used to supply the galvanizing finish.