Carbon Steel

OnGrip® Spray Traction Surface, as manufactured by Ohio Gratings, Inc. (800-321-9800) www.ohiogratings.com, shall be applied to the materials as shown on the drawings.  The OnGrip® Spray Traction Surface meets the American with Disabilities Act (ADA) requirement for slip resistance and OSHA safety standards.  The surface greatly exceeds the High Traction 0.42 Wet Dynamic Coefficient of Friction (DCOF) requirement of ANSI A137.1-2019 when tested per the ANSI A326.3 -2017 standard.  The metal spray is thermally applied to the carbon steel material surface covering 100% of the substrate surface. The surface has a minimum bond strength of 4,000 PSI when tested per ASTM D4541-2017.

Stainless Steel

OnGrip® Spray Traction Surface, as manufactured by Ohio Gratings, Inc. (800-321-9800) www.ohiogratings.com, shall be applied to the materials as shown on the drawings. The OnGrip® Spray Traction Surface meets the American with Disabilities Act (ADA) requirement for slip resistance and OSHA safety standards. The surface greatly exceeds the High Traction 0.42 Wet Dynamic Coefficient of Friction (DCOF) requirement of ANSI A137.1-2019 when tested per the ANSI A326.3 -2017 standard.  The metal spray is thermally applied to the stainless steel material surface covering 100% of the substrate surface. The surface has a minimum bond strength of 4,000 PSI when tested per ASTM D4541-2017.

Aluminum

OnGrip® Spray Traction Surface, as manufactured by Ohio Gratings, Inc. (800-321-9800) www.ohiogratings.com, shall be applied to the materials as shown on the drawings. The OnGrip® Spray Traction Surface meets the American with Disabilities Act (ADA) requirement for slip resistance and OSHA safety standards. The surface greatly exceeds the High Traction 0.42 Wet Dynamic Coefficient of Friction (DCOF) requirement of ANSI A137.1-2019 when tested per the ANSI A326.3 -2017 standard.  The metal spray is thermally applied to the aluminum material surface covering 100% of the substrate surface. The surface has a minimum bond strength of 3,000 PSI when tested per ASTM D4541-2017.